3.0mm Round Type LED Lamp

ATTENTION

OBSERVE PRECAUTIONS

FOR HANDLING

ELECTROSTATIC

SENSITIVE DEVICES

- Features :

- Choice of various viewing angles

- Available on tape and reel.

- Reliable and robust

- Pb free

- The product itself will remain within RoHS compliant version.

- Descriptions :

- The series is specially designed for

applications requiring higher brightness

- The led lamps are available with

different colors, intensities.

- Applications:

- TV set

- Monitor

- Telephone

- Computer

| PART NO. | Material | Emitting Color | Lens Color |
| --- | --- | --- | --- |
| 204SUWWC | InGaP | Warm White | Water Clear |
| 204SUWC | InGaP | White | Water Clear |

- Packing Dimensions & Spatial Distribution:

| Product Model | Emitting Color |  | LENS |  | DIE Material |  |
| --- | --- | --- | --- | --- | --- | --- |
| 204SUWWC/204SUWC | Warm White /White |  | Water Clear |  | InGaN |  |
| Tolerance Grade | Dimension Tolerance (UNIT: mm Tolerance ) |  |  |  |  |  |
|  | 0.5~3 | 3~6 |  | 6~30 |  | 30~120 |
| Medium(m) | ±0.1 | ±0.2 |  | ±0.3 |  | ±0.5 |

2. Absolute Maximum Ratings: (TA=25℃)

| Parameter | Symbol | Color | Maximum Rating | Unit |
| --- | --- | --- | --- | --- |
| Peak Forward Current | IFp | Warm/White | 70 | mA |
| Forward Current | IF | Warm/White | 20 | mA |
| Reverse Voltage | VR | Warm/White | 5 | V |
| Power Dissipation | Pd | Warm/White | 100 | mW |
| Operating Temperature | Topr | Warm/White | -40 ~ +85 | ℃ |
| Storage Temperature | Tstg | Warm/White | -40 ~ +85 | ℃ |
| Electrostatic Discharge | ESD | Warm/White | 1000 | V |
| Soldering Temperature | 260℃ for 5 seconds |  |  |  |

Notes:

1. Absolute maximum ratings Ta=25℃.

2. Tolerance of measurement of forward voltage±0.1V.

3. Tolerance of measurement of peak Wavelength±2.0nm.

4. Tolerance of measurement of luminous intensity±15%.

5. Tolerance of measurement of angle intensity±15%.

- Optical-Electrical Characteristic:(TA=25℃)

| Parameter | Symbol | Condition | Color | Min | Type | Max | Unit |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Forward Voltage | VF | IF=20mA | White | 3.0 | 3.3. | 3.6 | V |
| Reverse Current | IR | VR=5V | White | - | - | 10 | uA |
| Color Temp. | λd | IF=20mA | Warm White | 2800 | 3000 | 3500 | K |
| Color Temp. | λd | IF=20mA | White | 5500 | 6000 | 6500 | K |
| Luminous Intensity | Iv | IF=20mA | Warm White | 4000 | 4500 | 5000 | mcd |
| Luminous Intensity | Iv | IF=20mA | White | 4000 | 5000 | 6000 | mcd |
| Viewing Angle | 2θ1/2 | IF=20mA | White | - | 15 | - | deg |

- Reliability Performance Testing)：

Test Items & Result

| Type | Test Item | Ref. Standard | Test Conditions | Note | Number of Damaged |
| --- | --- | --- | --- | --- | --- |
| Environmental Sequence | Resistance to Soldering Heat | JESD22-B106 | Tsld=260℃,10sec | 2 times | 0/22 |
|  | Temperature Cycle | JESD22-A104 | -40℃ 30min ↑↓ 5min 100℃ 30min | 100 cycle | 0/22 |
|  | Thermal Shock | JESD22-A106 | -40℃ 15min ↑↓ 100℃ 15min | 100 cycle | 0/22 |
|  | High Temperature Storage | JESD22-A103 | Ta=100℃ | 1000 hrs | 0/22 |
|  | Low Temperature Storage | JESD22-A119 | Ta=-40℃ | 1000 hrs | 0/22 |
|  | Power temperature Cycling | JESD22-A105 | On 5min -40℃>15min ↑ ↓ ↑ ↓<15min Off5min 100℃>15min | 100 cycle | 0/22 |
| Operation Sequence | Life Test | JESD22-A108 | Ta=25℃ IF=30mA | 1000 hrs | 0/22 |
|  | High Humidity Heat Life Test | JESD22-A101 | 60℃ RH=90% IF=20mA | 1000 hrs | 0/22 |

Typical Optical/Electrical Characteristics Curves

(Ta=25℃ Unless Otherwise Noted)

- Soldering:

1. Manual of Soldering

The temperature of the iron tip should not

be higher than 260℃(500℉) and Soldering

within 3 seconds per solder-land is to be

observed.

2. DIP soldering (Wave Soldering):

Preheating:120℃~150℃,within 120~180 sec.

Operation heating:245℃±5℃

within 5 sec.260℃(Max)

Gradual Cooling (Avoid quenching).

- Handling:

Care must be taken not to cause to the epoxy resin portion of LED while it is exposed to high temperature.

Care must be taken not rub the epoxy resin portion of LED with hard or sharp article such as the sand blast and the metal hook.

Care must be taken there should be more than 3mm from jointing point to the epoxy resin.

- Notes for designing:

Care must be taken to provide the current limiting resistor in the circuit so as to drive the LED within the rated figures .Also caution should be taken not to overload LED with exorbitant voltage at the turning ON and OFF of the circuit.

When using the pulse drive care must be taken to keep the average current within the rated figures .Also the circuit should be designed so as be subjected to reverse voltage when turning off the LED.

- Storage:

In order to avoid the absorption of moisture. It is recommended to solder LED as soon as possible after unpacking the sealed envelope.

If the envelope is still packed to store it in the environment as following:

Temperature:-5℃~45℃(23℉~113℉), Humidity : RH 60% Max.