Technical    Data    Sheet

Product Name：PLCC-5050 High Bright Red SMD Chip LED

Part Number：      HT61-2301SURSURSURC(S)

Customer：

Customer PN：

Version No.：                  A.2

Date：                            2009.01.01

Customer Approval

1、Features

	Package ( L/W/H ) : 5.4 × 5.0 × 1.6 mm

	Color :    Ultra Bright Red

	Lens: Water Clear Flat Mold

	EIA STD Package

	Meet ROHS, Green Product

	Compatible With SMT Automatic Equipment

	Compatible With Infrared Reflow Solder And Wave Solder Process

2、  Package Profile & Soldering PAD Suggested

+	①

+	③

+	⑤

MARK

Φ3.3

② -

④ -

⑥ -

+	①

+	③

+	⑤

Polatity

②  -

④  -

⑥  -

Notes:    1. All dimensions are in millimeters ;

2. Tolerance is ± 0.10 mm unless otherwise noted.

3、  Soldering Profile Suggested

3.1、For Lead Solder

3.2、For Lead Free Solder

4．  Absolute    Maximum    Ratings    At    Ta=25℃

Parameter	Symbol

R1

Rating

70

Unit

Power Dissipation

Peak Forward Current

(1/10 Duty Cycle, 0.1ms Pulse Width)

DC Forward Current

Reverse Voltage

Operating Temperature Range

Pd

IFP

IF

VR

Topr

R2

R3

R1

R2

R3

R1

R2

R3

R1

R2

R3

70

70

70

70

70

30

30

30

5

5

5

-30°C    ~    + 85°C

mW

mA

mA

V

Storage Temperature Range

Soldering Condition

Tstg

Tsol

-40°C    ~    + 90°C

Reflow soldering : 260°C For 5 Seconds

Hand soldering: 300°C For 3 Seconds

5、  Electrical    Optical    Characteristics    At    Ta=25℃

Parameter	Symbol 	Color	Min.	Typ.	Max.

Unit

Test Condition

Luminous Intensity

Dominant Wavelength

Peak Wavelength

Spectral Line Half-Width

Forward Voltage

IV

λd

λp

Δλ

VF

R1

R2

R3

R1

R2

R3

R1

R2

R3

R1

R2

R3

R1

R2

R3

---

---

---

---

---

---

---

---

---

---

---

---

1.8

1.8

1.8

280

280

280

624

624

624

630

630

630

20

20

20

---

---

---

---

---

---

---

---

---

---

---

---

---

---

---

2.6

2.6

2.6

mcd

nm

nm

nm

V

IF = 20mA

IF=20mA

IF=20mA

IF=20mA

IF=20mA

R1	---	---	10

Reverse Current	IR	R2	---	---	10	uA

VR=5V

Viewing Angle

2θ1/2

R3

---

---

---

---

120

10

---

deg

IF = 20mA

Notes: 1. Luminous intensity is measured with a light sensor and filter combination that approximates the

CIE eye-response curve.

2. θ1/2 is the off-axis angle at which the luminous intensity is half the axial luminous intensity.

3. The dominant wavelength, λd is derived from the CIE chromaticity diagram and represents the

single wavelength which defines the color of the device.