Technical    Data    Sheet

Product Name：PLCC-5050 Green SMD Chip LED

Part Number：      HT61-2301UBGUBGUBGC(S)

Customer：

Customer PN：

Version No.：                  A.2

Date：                            2009.01.01

Customer Approval

Instituted By：                              Checked By:                                Approved By：

1、Features

	Package ( L/W/H ) : 5.4 × 5.0 × 1.6 mm

	Color : Ultra Bright Green

	Lens: Water Clear Flat Mold

	EIA STD Package

	Meet ROHS, Green Product

	Compatible With SMT Automatic Equipment

	Compatible With Infrared Reflow Solder And Wave Solder Process

2、  Package Profile & Soldering PAD Suggested

①

③

⑤

MARK

Φ3.3

②

④

⑥

Notes:    1. All dimensions are in millimeters ;

2. Tolerance is ± 0.10 mm unless otherwise noted.

3、  Soldering Profile Suggested

3.1、For Lead Solder

3.2、For Lead Free Solder

2 of 10

Technical    Data    Sheet

Part No. :    HT61-2301UBGUBGUBGC(S)

Version	A.2	Issued date	2009.01.01	Page

4．  Absolute    Maximum    Ratings    At    Ta=25℃

3 of 10

Parameter

Power Dissipation

Symbol

Pd

G1

G2

G3

Rating

90

90

90

Unit

mW

Peak Forward Current

(1/10 Duty Cycle, 0.1ms Pulse Width)

DC Forward Current

Reverse Voltage

Operating Temperature Range

Storage Temperature Range

IFP

IF

VR

Topr

Tstg

G1

G2

G3

G1

G2

G3

G1

G2

G3

100

100

100

30

30

30

5

5

5

-30°C    ~    + 85°C

-40°C    ~    + 90°C

mA

mA

V

Soldering Condition

Tsol

Reflow soldering : 260°C For 5 Seconds

Hand soldering: 300°C For 3 Seconds

Technical    Data    Sheet

Part No. :    HT61-2301UBGUBGUBGC(S)

Version	A.2	Issued date	2009.01.01	Page

5、  Electrical    Optical    Characteristics    At    Ta=25℃

4 of 10

Parameter

Symbol

Color

G1

Min.

---

Typ.	Max.

1000	---

Unit

Test Condition

Luminous Intensity

Dominant Wavelength

Peak Wavelength

Spectral Line Half-Width

Forward Voltage

Reverse Current

Viewing Angle

IV

λd

λp

Δλ

VF

IR

2θ1/2

G2

G3

G1

G2

G3

G1

G2

G3

G1

G2

G3

G1

G2

G3

G1

G2

G3

---

---

---

---

---

---

---

---

---

---

---

---

2.8

2.8

2.8

---

---

---

---

1000

1000

525

525

525

530

530

530

35

35

35

---

---

---

---

---

---

120

---

---

---

---

---

---

---

---

---

---

---

3.6

3.6

3.6

10

10

10

---

mcd

nm

nm

nm

V

uA

deg

IF = 20mA

IF=20mA

IF=20mA

IF=20mA

IF=20mA

VR=5V

IF = 20mA

Notes: 1. Luminous intensity is measured with a light sensor and filter combination that approximates the

CIE eye-response curve.

2. θ1/2 is the off-axis angle at which the luminous intensity is half the axial luminous intensity.

3. The dominant wavelength, λd is derived from the CIE chromaticity diagram and represents the

single wavelength which defines the color of the device.