Characteristics

- Application

      - Advertisement

      - Indicators

      - Back Lights

      - Illumination

      - High-Brightness LED

      - Lens Color :  YELLOW

      - Half Angle(2θ1/2) :120°

      - Superior Weather-resistance

      - UV Resistant Epoxy

- Directivity                                ■Outline Dimension

■ Electrical Optical Characteristics

| Item | Symbol | Min. | Typ. | Max. | Unit | Condition |
| --- | --- | --- | --- | --- | --- | --- |
| # Luminous Intensity | Iv | 350 | --- | 500 | mcd | IF=20mA |
| Viewing Angle | 2θ1/2 | --- | 120 | --- | Deg |  |
| Wave length | WLD | 587 | --- | 593 | -- |  |
| ##### Forward Voltage | VF | 1.9 | --- | 2.1 | V |  |
| Reverse Current | IR | --- | --- | 5 | μA | VR=5V |

  - Please Refer to CIE 1931 chromaticity diagram

- Absolute Maximum Rating

| Item | Symbol | Maxabsolute | Unit |
| --- | --- | --- | --- |
| #### Power Dissipation | PD | 100 | mW |
| Peak forward current(1/10 duty cycle,0.1ms pulse width | IFP | 50 | mA |
| Continuous forward current | IF | 20 | mA |
| Derating linear from 50℃ |  | 0.4 | mA/℃ |
| Reverse voltage | VR | 5.0 | V |
| Operating temperature range | Topr | -40℃ to +80℃ |  |
| Storage temperature range | Tstg | -40℃ to +100℃ |  |
| soldering temperature | Tsod | 260℃ for 3 Seconds |  |

- Pulse width Max 10ms Duty ratio Max 1/10

- Optical Electrical Characteristics